Section 403 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The first sentence of Subsection 403.03(e) is hereby deleted and the following substituted therefore:

Polymer Modified (CRS-2P) and Latex Modified (CRS-2L) Cationic Emulsified Asphalt shall conform to the requirements of AASHTO M 316, except for the minimum Ductility at 25º C (77ºF).

Item 2) of the last sentence of Subsection 403.03(e) is hereby deleted and the following substituted therefore:

2) The minimum residue from evaporation by weight shall be 68%, and