Section 303 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The sixth paragraph of Subsection 303.02 is hereby deleted and the following is substituted therefore:

For Classes 1 through 8 material, the fraction passing the #200 (0.075 mm) sieve shall not be greater than three-fourths of the fraction passing the #40 (0.425 mm) sieve.  For Classes 3 through 8 the fraction passing the #40 (0.425 mm) sieve shall have a liquid limit not greater than 25.

Table 303-1, Aggregate Base Course Grading, is hereby amended by deleting the percent passing the No. 200 (0.075 mm) sieve gradation for Classes 6, 7, and 8 and the following substituted therefore:

The percent passing the No. 200 (0.075 mm) sieve grading for Classes 6, 7, and 8 will be 3 – 12.