Section 404 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The third and fourth paragraphs of Subsection 404.04, Quality Control of Asphalt Mixtures, are hereby deleted and the following substituted therefore:

The accepted mix design shall be field verified by the Contractor at the start of mix production or after an interruption of more than 90 calendar days.  The asphalt mixture shall be verified by testing mix that has been produced through the plant using the aggregate proportions shown on the accepted mix design.

The mix will be considered to be verified if test values for air voids, VMA, and asphalt binder content are within the compliance limits shown in Table 410-1, and when the accepted mix design has been produced within the gradation tolerances according to Subsection 404.04.