Table 409-1 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

Table 409-1

Coarse Aggregate Properties

| Coarse Aggregate Type Size Fractured Faces One Face Two Faces LA Abrasion (AASHTO T 96) Sodium Sulfate Soundness (AASHTO T 104, 5 cycle) Flat, Elongated Particle Wearing Surface Aggregate Limestone Other Note 1 Gravel Other Note 2 | Crushed Gravel; Crushed Stone; Crushed Steel Slag Plus No. 8 (2.36 mm) 98 % min. 80 % min. 40 % max. 12% max. 10 % max. 60 % max. 40 % min. 60 % max. 40 % min. |
| --- | --- |

Note 1: Crushed sandstone, crushed siliceous gravel, syenite, novaculite, crushed steel slag or mineral aggregate which has an insoluble residue not less than 85% when tested in a 1:1 solution of hydrochloric acid and water according to AHTD Test Method 306 shall be used as the remaining coarse mineral aggregate.

Note 2: Crushed steel slag, crushed sandstone, syenite, novaculite, or other crushed quarry stone which has an insoluble residue not less than 85% when tested in a 1:1 solution of hydrochloric acid and water according to AHTD Test Method 306 shall be used as the remaining coarse mineral aggregate.