Section 411 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The second paragraph of subsection 411.02(a) is hereby deleted and the following substituted therefore:

The asphalt shall be an MC-250, MC-800, MC-3000, a summer or winter grade seasonal type asphalt, or an inverted emulsion type asphalt.

The following is added at the end of the fourth paragraph of subsection 411.02(a):

Inverted emulsion type asphalt shall comply with the following requirements:

- Inverted emulsions

Characteristics						Minimum	Maximum

-Flash Point, Tag Open Cup oF			    200		       ----

-Viscosity (SF), sec at 140oF 				    100		       ----

(AASHTO T 59)

-Stone CoatingA

Coating, %					      90		       ----

Asphalt Run-off, %				     ----	          	          0

-Test on Residue from Distillation

500oF (AASHTO T 59)

Residue by Distillation, % by Mass		      80		       ----

Oil Distillate, % by Volume			        2		       ----

-Test on Residue from Cutback Distillation

(AASHTO T 78)

Absolute Viscosity, P (AASHTO T 202)	      30		      800

Solubility, % (AASHTO T 44)		   97.5		       ----

A - Stone Coating Test (at 140F)

- Weigh 200 grams of dry aggregate (at the gradation of the mix design) into a beaker.

- Weigh 4 grams of distilled water into the beaker containing the dry aggregate and mix for 30 seconds.

- Dose dry aggregate w/ inverted emulsion at optimum AC% and add to the beaker containing the damp aggregate and mix vigorously for 120 seconds.

- Dump contents in beaker onto a metal pan or suitable surface and visually check coating of aggregate.  There shall be no evidence of asphalt run-off.

The requirement “Mineral Filler 3.0% minimum” of Table 411-1, Design Requirements for Asphalt Concrete Cold Plant Mix, is hereby deleted.