Section 604 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The first two paragraphs of Subsection 604.02(b) are hereby deleted and the following substituted therefore:

(b) Signs, Vertical Panels, Barricades, Drums and Traffic Cones.  Materials for signs required under this subsection shall comply with materials requirement of the plans, specifications and the MUTCD for the construction of signs using ASTM D 4956 Type VII, VIII, or IX sheeting for non-orange signs and Fluorescent Orange retroreflective sheeting furnished according to the QPL for orange signs.  Materials for vertical panels and barricades shall comply with ASTM D 4956 Type VII, VIII, or IX sheeting.

Retroreflective sheeting used on traffic drums shall meet the requirements of ASTM D4956 for Type III or Type IV with the additional requirements for Reboundable Sheeting.  Retroreflective sheeting for delineators shall meet the requirements of ASTM D 4956 for Type IX sheeting.

Table 604-1 Fluorescent Orange Sheeting and Table 604-2 Fluorescent Orange Color Specification Limits (Daytime) in Subsection 604.02(b) are hereby deleted and the following substituted therefore:

## TABLE 604-1

# Fluorescent Orange Sheeting

|  | Minimum Coefficient Of Retroreflection Candelas Per Foot Candle Per Square Foot |  |
| --- | --- | --- |
| Observation Angle | Entrance Angle | Fluorescent Orange |
| 0.2 | -4.0 | 200 |
| 0.2 | 30.0 | 92 |
| 0.5 | -4.0 | 80 |
| 0.5 | 30.0 | 30 |

TABLE 604-2

Fluorescent Orange Color Specification Limits (Daytime)

| Corner Point: | 1 |  | 2 |  | 3 |  | 4 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | x | y | x | y | x | y | x | y |
|  | 0.583 | 0.418 | 0.516 | 0.397 | 0.560 | 0.341 | 0.655 | 0.345 |