Section 606 of the Standard Specification for Highway Construction, Edition of 2003, is hereby amended as follows:

The fifth paragraph of Subsection 606.02 Materials (b) Reinforced Concrete Pipe is hereby deleted and the following substituted therefor:

(4) Joints shall be sealed with either preformed rubber gaskets or bitumen/ butyl rubber plastic gaskets complying with AASHTO M 198 or with tubular cross-section closed cellular rubber gaskets complying with the physical requirements of ASTM D 1056 (Type 2, Class C, Grade 1) and meeting the chemical requirements of AASHTO M 198.

The sixth paragraph of Subsection 606.03 Construction (d) Joining Pipe is hereby deleted and the following substituted therefore:

(3) When tubular cross-section closed cellular rubber gaskets are selected by the Contractor, the gaskets shall be a single, continuous part conforming to the joint shape.  The outer surface of the gasket shall be completely covered with a natural skin.  The cross-sectional diameters and installation practices shall be in accordance with the manufactures’ recommendations for the size of pipe or culvert being placed.

To ensure an even and well-filled joint, the final joining of the pipe shall be accomplished by either pushing or pulling, by approved mechanical means, each joint of the pipe as it is laid.  In cold weather, when directed, the joint material shall be warmed in a hot water bath, or by other approved methods, to the extent required to keep the material pliable for placement without breaking or cracking.