Section 718 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The first paragraph of the Subsection 718.02 Materials of the Standard Specifications for Highway Construction, Edition of 2003, is hereby deleted and the following substituted therefore:

718.02 Materials.  The paint shall be a ready mixed white and yellow paint suitable for application on concrete and bituminous pavements.  All paints used for this application shall be listed on the QPL.  The manufacturer shall furnish a certification for each lot certifying that the materials supplied conform to all the requirements specified and stating that the material is formulated the same as the material tested for QPL listing.  Random samples may be taken and tested by the Department.  The paint shall be a solventborne-chlorinated rubber, solventborne chlorinated polyolefin, solventborne acrylic copolymer, a waterborne acrylic emulsion polymer paint or a cold weather waterborne acrylic emulsion polymer paint.

The following is added to the third paragraph of the Subsection 718.02 Materials of the Standard Specifications for Highway Construction, Edition of 2003:

Cold weather waterborne acrylic emulsion polymer paint does not have to meet the Raw Materials requirements of paragraph (d), Raw Materials for Vehicles (Waterborne), or subparagraphs (1) and (2) of paragraph (f) Physical Requirements of the Finished Pavement (Waterborne).

Subsection 718.02 Materials, (a), (5) of the Standard Specifications for Highway Construction, Edition of 2003, is hereby deleted and the following substituted therefore:

The pigments used for the pavement marking material compound shall not contain any compounds that will exceed the values listed in the Environmental Protection Agency Code of Federal Regulations (CFR) 40, Section 261.24, Table 1.