Section 719 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The second paragraph of Subsection 719.02 is hereby deleted and the following substituted therefore:

The material shall meet the requirements of AASHTO M 249 with the following exceptions for color on yellow materials.

Color Specifications

| Color Specification Limits -Daytime Initial |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Chromaticity Coordinates |  |  |  |  |  |  |  | Luminance Factor, Y(%) |  |
| 1 |  | 2 |  | 3 |  | 4 |  | min | max |
| x | y | x | y | x | y | x | y |  |  |
| 0.499 | 0.466 | 0.545 | 0.455 | 0.518 | 0.432 | 0.485 | 0.454 | 40.0 | 60.0 |

Initial daytime color determination will be made in accordance with the requirements of AASHTO T 250.  Values shall be evaluated on material without the drop-on beads.

| Color Specification Limits -Daytime Retained |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Chromaticity Coordinates |  |  |  |  |  |  |  |
| 1 |  | 2 |  | 3 |  | 4 |  |
| x | y | x | y | x | y | x | y |
| 0.560 | 0.440 | 0.490 | 0.510 | 0.420 | 0.440 | 0.460 | 0.400 |

Retained daytime color limits shall conform to the specifications for a minimum of ninety days for construction pavement markings and one year for all other markings.  Retained readings will be determined on a beaded surface in accordance with the requirements of ASTM E 2366.

| Color Specification Limits -Nighttime Initial with drop-on beads |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Chromaticity Coordinates |  |  |  |  |  |  |  |
| 1 |  | 2 |  | 3 |  | 4 |  |
| x | y | x | y | x | y | x | y |
| 0.575 | 0.425 | 0.508 | 0.415 | 0.473 | 0.453 | 0.510 | 0.490 |

Initial nighttime color limits will be determined in accordance with the requirements of ASTM E 2367 on a beaded surface.

The pigments used for the pavement marking material compound shall not contain any compounds that will exceed the values listed in the Environmental Protection Agency Code of Federal Regulations (CFR) 40, Section 261.24, Table 1.