Section 723 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The first paragraph of Subsection 723.02 Materials and Fabrication. (c) Retroreflective Sheeting is hereby deleted and the following substituted therefore:

The retroreflective sheeting for signs and delineators shall comply with ASTM D 4956 for Type III, VIII or IX Retroreflective Sheeting, except that Type VIII or Type IX Retroreflective Sheeting shall be used on all delineators.  All retroreflective sheeting shall have either Class 1 or Class 2 backing.

The second paragraph of Subsection 723.02 Materials and Fabrication. (d) Legend. (2) Demountable Legend is hereby deleted and the following substituted therefore:

Frames for border strips, corners, legend and shields shall be fabricated from 0.063” (1.6mm) sheet aluminum complying with the requirements of ASTM B 209, Alloy 5052-H38.