## Slide 1
Presented in cooperation with the National Asphalt Pavement Association.
Larry Patrick
Executive Director
Oklahoma Asphalt Pavement Association

## Slide 3: Thinlay – What is it?
Group of asphalt mixes that can be placed at a depth of 5⁄8 inch or more.
Designed for pavement preservation

## Slide 4: Benefits of Thin Asphalt Overlays
Long life and low life-cycle cost!
Safety / User
  Minimize traffic delays
  Staged construction
  Smooth surface
  Restore skid resistance
  No loose stones & minimizes dust
  Lower noise
Structural
  Maintain grade & slope
  Withstands heavy traffic
  Easy to maintain
  Add structure
Sustainable
  Recycled materials
  Seals surface & no binder run-off
Versatile
Notes: Thin asphalt overlays have a number of advantages for their usage. Most importantly they provide a long life and low life-cycle cost. Their application provides a means of maintaining the grade and slope of a pavement eliminating the need for deep excavation and unnecessary handwork. They can be designed for any traffic condition from car parking lots to freeways and commercial development. They have no loose stones and minimize dust after application unlike some other types of pavement preservation treatments. There is no need for a curing time prior to allowing traffic. Binder does not run off the pavement at the time of application or soon thereafter. They provide a quiet pavement surface. The asphalt mixture can be recycled at the end of its performance life. Thin overlays have been effectively used in stage construction. And, finally, they are easy to place and maintain with minimal traffic disruption. Thin asphalt overlays will also enhance the pavement’s appearance and helps to seal the pavement from oxidation and moisture.

## Slide 5: Structural Benefits
Preventive Maintenance treatments are typically non-structural
Preventive Maintenance treatments should be applied to structurally sound pavements
Slurry seals, Chips Seals, micro surfacing add no structure
A 1 inch Thinlay asphalt treatment does provide structural benefits

## Slide 6: Structural Benefits
Most in-service pavements were designed for 20 years with AASHTO design
They have finite bottom up fatigue life, meaning if thickness is not increased the pavement will eventually fail from bottom up cracking
TENSILE STRAIN

## Slide 7: Structural Benefits
A seal type treatment applied on those pavements will have no impact on the tensile strain and therefore no impact on the structural life
TENSILE STRAIN

## Slide 8: Structural Benefits
Preventive seals on these pavements will only mask the impending structural distresses and eventually lead to full depth failures

## Slide 9: Timely Thinlay treatments can save your structure

## Slide 10: Thinlay Structure?

## Slide 11
Thickness | Micro strain | Reps to failure
2 | -652 | 30,234
3 | -495 | 71,537
4 | -383 | 160,693
5 | -302 | 340,507
6 | -242 | 682,133
What’s in an inch?
Asphalt Thickness VS. Fatigue Life

## Slide 12: Perpetual 1” at a time
The goal of a perpetual pavement is to achieve a thickness that will confine future distresses to the surface
Full depth failures are prevented
The pavement can than be managed at the surface indefinitely

## Slide 13: Washington State - Top-Down in Asphalt Pavements > 150 mm
150 mm
50 mm
Notes: In Washington state, it was found that longitudinal cracks in pavements with HMA layers of 6 inches or more started at the surface and propagated only two to three inches into the structure.

## Slide 14: Perpetual 1” at a time
A properly designed (20 year) pavement can get to perpetual by adding 2 inches and getting total thickness of 6 inches or more

## Slide 15: Structural contribution of 1”
A 1 inch overlay of an existing 4 inch pavement will double the fatigue life
A second 1 inch overlay can extend the structural life beyond 50 years
Once you achieve a perpetual thickness you can focus on managing at the surface for functional attributes as your structural worries are over

## Slide 16: Project Selection
Avoid Projects Needing Structural Rehabilitation!!
Notes: Not every pavement project is suitable for a thin asphalt overlay. It is best to apply a thin overlay prior to the need for a more extensive pavement rehabilitation.

## Slide 17: Visual Survey
Part of a good Pavement Management System.
Get current project-specific data
Need to know:
  Type of distress
  Extent
  Severity
Visit the site and validate data.
Notes: A visual survey of the pavement condition is usually included as part of a pavement management system that is often used to determine whether a preservation, rehabilitation or reconstruction is necessary. Because this information may be years old it is important to gather current project-specific data to make sure the proposed preservation strategy is viable. The survey should include the type of distress present in the pavement along with the extent and severity. This survey can normally be done through a windshield survey by two persons rather than the platoon of pavement raters shown here!

## Slide 18: Types of Distress
Raveling
Longitudinal Cracking (not in wheelpath)
Longitudinal Cracking (in wheelpath)
Transverse Cracking
Alligator Cracking
Rutting
Notes: These are common distress that are usually identified by standard distress surveys. (read list)
There is also an FHWA Long Term Pavement Performance (LTPP) program manual available for visually identifying pavement distresses.

## Slide 19: Raveling
Notes: Raveling is recognizable as a loss of fine aggregate on the pavement surface, which can be followed by loss of the coarse aggregate.
Raveling is normally readily fixed by a thin asphalt overlay, even if it is relatively severe. It is important to catch it before the extensive pavement deterioration. Mouse Click to show check mark
Optional: One word of caution is that when the raveling is due to moisture susceptibility. Thin dense-graded overlays can seal the pavement causing stripping in the lower level that may lead to rutting. It is probably best to mill the layer prior to overlay in this case.

## Slide 20: Longitudinal Cracking (not in wheelpath)
Notes: Longitudinal cracking that is not located in the wheelpath can usually be considered a good candidate for a thin asphalt overlay. The thin overlay should be applied prior to the extensive deterioration of the crack. A thin overlay will help to seal the surface so that water cannot so easily penetrate and further damage the crack.
Mouse Click to show check mark

## Slide 21: Longitudinal Cracking (wheelpath)
Temporary Fix for Minor Distress
Notes: If longitudinal cracking occurs within the wheel path, it is a little trickier. If the crack is starting at the surface and progressing down it is a good candidate for a thin overlay. Because top down cracking growth slows dramatically with depth and thin overlay can be very effective here. Mouse Click to show check mark
However, if this crack is progressing from the bottom up it may signal the beginning of some fatigue cracking. While a thin overlay may help temporarily, it should be noted that most likely the crack will eventually propagate through the overlay, and the structural deterioration of the pavement will continue. Remember, a thin overlay does not cure structural problems.
The only way to determine if this is bottom up or top down cracking is to take a core at the location of (through) the crack.

## Slide 22: Transverse Cracking
Notes: Pavements with low to medium transverse cracking are often suitable for a thin overlay, especially if the overlay is applied prior to severe cracking. If caught early enough, the existing pavement can be merely overlaid, or, if it has progressed beyond its initial stage, the pavement can be milled to a depth below the crack and the thin overlay will have the opportunity to avoid or reduce reflective cracking. If the cracking is deep, say more than 50 percent of the asphalt depth the pavement may be milled just to reduce the crack width prior to overlay placement.
Mouse Click to show check mark

## Slide 23: Alligator (Fatigue) Cracking
Temporary Fix for Minor Distress
Notes: A thin asphalt overlay is not recommended for a fatigue cracked pavement. This requires a structural rehabilitation which includes fixing the failure prior to the placement of a structural overlay.
Mouse Click to show red circle
Optional: If the fatigue cracking is only in isolated areas – full depth patching of the fatigue cracked areas should be conducted prior to overlay.

## Slide 24: How deep is the crack?
New Jersey I-287 Surface Cracking
Notes: This slide shows the top-down cracking in New Jersey’s I-287, and how it stopped only a few inches into the pavement structure.
It is interesting to note that this cracking was shallow despite the appearance of severe deterioration on the pavement surface.
Non-destructive deflection testing confirmed that the pavement was structurally sound and that only surface milling with an overlay was necessary to restore the riding characteristics.

## Slide 25: Rutting or Shoving
Surface Failure –
Milling Required
Severe Structural Failure
Notes: A thin overlay can be used on a rutted pavement so long as the rutting is not structural in nature and the in-place mixtures below the surface layer are properly designed and performing well. Leveling, shimming or milling may be necessary for deeper ruts.
Mouse Click to show text below right picture
For example, if the distress is on the surface, then the wheelpaths will be very clearly defined as in the right hand picture. In this case, milling to remove the defective surface and replacement with a thin overlay should work very well.
Mouse Click to show check mark
Mouse Click to show check text below left picture
If it is structural, then the problems have origins fixed deep in the pavement structure, the rut is relatively broad, and the rehabilitation will have to begin with fixing the structural problem. This is shown in the left hand picture.
Mouse Click to show check mark
Optional: The only way to truly know what layer is responsible for rutting is to cut a trench across the roadway and do a series of cores across the roadway to determine which layer is responsible for the deformation.

## Slide 26: Noise can be reduced
Chart: NCAT Noise Trailer
| 9.5 mm (Rt. 50) | 12.5 mm (I-270) | 12.5 mm (I-495) | 19 mm (I-83)
 | 95.5 | 97.7 | 98.9 | 99
Smaller Aggregate = Less Noise
Notes: One of the advantages of thin overlays when it comes to tire-pavement noise is that they often use small aggregate size. Mixes that use smaller maximum aggregates are typically quieter than mixes with larger stone. This is illustrated in this graph from a Maryland study on tire-pavement noise. You can see that the noise level can be reduced by more than 4 decibels by reducing the nominal maximum aggregate size from
19 mm to 9.5 mm.
Mouse Click to show arrow and text at bottom
A reduction of 3 decibels has the same impact on noise as reducing the traffic by half.

## Slide 27: Mix Types
Dense-Graded
Stone Matrix Asphalt (SMA)
Open-Graded

## Slide 28: How do you select the mix type for a thin overlay?
Notes: There are a number of mix types that may be used for thin overlays. The type selected depends on many factors including traffic, environment and even aesthetics. One guide that can help in selecting mix types is shown here. It was a joint project of NAPA and the Federal Highway Administration.

## Slide 29
Recommended Mix Types Surface Courses
Low Traffic
Medium Traffic
High Traffic
Notes: Here is one chart that is used in the publication to help determine what type of mix is appropriate for different traffic levels. The mixes are broken down by mix type.
DFG – Dense fine graded
SMA – Stone Matrix Asphalt
OGFC – Open graded friction course
And DCG – Dense coarse graded mixes.
One may note here that dense fine graded mixes are not recommended for high traffic situation. This publication was developed early in the Superpave mix design system when it was felt the coarse graded mixes would be better for high traffic. However, we now know through experience and research that the fine graded mixes are more than up to the task of high traffic volumes.
Click mouse for animation
Therefore, the chart should really look more like this now.

## Slide 30: If a Thinlay is the answer, you need to decide:
Surface Preparation
  Distresses
  Roughness
  Considerations for Curb Reveal and Drainage
Materials
  Traffic
  Availability
  Climate
Thickness
  NMAS
  Geometrics
Notes: Once the determination has been made that a thin asphalt overlay is appropriate, then decisions must be made regarding surface preparation, materials, and overlay thickness.
Surface preparation will be dependent upon the distresses present in the existing pavement, the need to correct roughness problems, drainage and geometric considerations.
The types of materials used in the thin overlay will depend upon the level of traffic expected, availability, and the climate of the particular project.
Since we are not trying to correct structural deficiencies with thin overlays, the thickness of the overlay will depend upon the nominal maximum aggregate size used in the overlay and geometric demands of the pavement surface.

## Slide 31: Surface Preparation
 | Mill | Fill Cracks with Mix | Clean and Tack
Raveling |  |  | 
Long. Crack – not in w.p. |  |  | 
Long. Crack – w.p. |  |  | 
Transverse Crack |  |  | 
Alligator Crack |  |  | 
Rutting |  |  | 
Notes: Surface preparation is project specific
Milling the pavement surface can be done for all types of pavement distresses, depending upon the project conditions. For example milling may be done to reduce or eliminate the chance for reflective cracking, improve smoothness, or remove rutted layers. The increased performance of a thin overlay over a milled surface may offset any extra costs. Remember the asphalt removed from the project is not wasted. It can be recycled back into new, high quality pavements saving valuable resources which includes dollars.
Crack filling with an asphalt mixture is suggested for longitudinal cracking and transverse cracking, but only if the cracking is severe enough to allow for filling and prevent dipping of the overlay. Liquid crack filler material can be problematic, especially with hot mix material as it may expand and cause bumps. Warm mix asphalt has been demonstrated to help solve this problem. Remember that milling may also be beneficial for eliminating or reducing reflective cracking
Although cleaning and tacking are shown to be recommended for all types of pavement distress, there are studies that show that milling by itself may be just as effective or more so than cleaning and tacking the pavement surface. However, when in doubt – tack.

## Slide 32: Thinlay Examples
Ohio Smoothseal
  Type A - recipe (all traffic)
    PG 76-22 (8.5% SBS)
    PG 64-22 (5.5% SBR)
    Thickness 5/8” < thickness < 1 1/8”
  Type B – volumetrics
    ½-inch max. sized coarse agg.
    min. polymer binder content of 6.4%
    PG 76-22 (8.5% SBS)
    PG 64-22 (5.5% SBR)
    Thickness: 3/4” < thickness < 1 1/2”
  “They should last 12 to 15 years, if they’re placed on the right pavement.” ODOT

## Slide 33: Thinlay Examples
New Jersey (5 Tools)
  high-performance thin overlay (HPTO)
    100% passing 3/8”
    PG 64E-22
    APA for mix design and production
    No RAP/RAS
    Minimum 7% AC
  ultra-thin friction course
    100% passing ½”
    PG 64E-22
    AC 4.9-6.0%
    No RAP
  stone-matrix asphalt (SMA) 9.5-mm surface course
  modified open-graded surface course (MOGFC)
  asphalt rubber open-graded friction course

## Slide 34: Texas TOM and UT Mixes

## Slide 35: Texas TOM and UT Mixes

## Slide 36: Materials Selection - RAP
Small NMAS mixes should utilized fine RAP
RAP or RAS will help
  Stabilize cost by reducing added asphalt and added aggregate
  Prevent rutting
  Prevent scuffing
Use maximum allowable while maintaining gradation and volumetrics
Notes: The use of reclaimed asphalt pavement in a thin overlay should be encouraged if the RAP is sized appropriately. Small size RAP can be very beneficial to the performance and cost of the mix, especially since the fine RAP will contain a higher amount of asphalt than coarser RAP.
Click mouse button to show arrow below finer RAP.
Reclaimed asphalt shingles (RAS) are also beneficial in thin overlays. RAS has a high percentage of asphalt binder. Between 20 and 30 percent. So even a low percentage of RAS may significantly reduce the amount of new asphalt binder required for a mix. Like RAP this stabilizes the cost of the mix, and the high temperature stiffening effect will prevent or reduce rutting and scuffing.
The approach in mix design should be to use the maximum amount of RAP and RAS while maintaining the gradation of the aggregate and mix volumetrics.

## Slide 37: 45% RAP

## Slide 38: 45% RAP

## Slide 39: NAPA/SAPA PEC Thinlay w/ High RAP
Chart: Oregon Overlay Test Results
| OR 12.5 30/0 64-22 | OR 4.75 30/0 64-22 | OR 4.75 40/0 58-28 | OR 4.75 40/0 58-34 | OR 4.75 50/0 58-34
Load Reduction, Cycles to Failure | 162 | 207 | 339 | 612 | 65
Normalized Load x Cycles to Failure | 44 | 68.6667 | 63.6667 | 235.6667 | 17

## Slide 40: NAPA/SAPA PEC Thinlay w/ High RAP
Chart: Oregon Overlay Test Results
| OR 12.5 30/0 64-28 | OR 4.75 30/0 64-28 | OR 4.75 40/0 58-28 | OR 4.75 40/0 58-34 | OR 4.75 50/0 58-34
Load Reduction, Cycles to Failure | 430.6667 | 356.6667 | 339 | 612 | 65
Normalized Load x Cycles to Failure | 186 | 154.6667 | 63.6667 | 235.6667 | 17

## Slide 41: NAPA/SAPA PEC Thinlay w/ High RAP
Chart: North Carolina Overlay Test Results
| 9.5 mm PG 64-22 30% RAP | 4.75 mm PG 64-22 50% RAP | 4.75 mm PG 58-28 50% RAP
MOD - 0.508 mm | 2759.3333 | 1777 | 1618.25
MOD - 0.635 mm | 599.3333 | 317.6667 | 658.5

## Slide 42: Permeability
Notes: This graph shows the results of a study NCAT conducted on the effect of air voids and nominal aggregate size on mix permeability in the field.
Click Mouse to circle 25 mm
Notice how high the permeability of this 25 mm mix is at even a relatively low air voids, and how rapidly this permeability chances as the air voids increase.
Click Mouse to circle 19 mm
As the nominal maximum aggregate size changes we can see a dramatic difference in the permeability of this 19 mm compared to the 25 mm mix at the same air voids.
Click mouse to circle 12 & 9.5 mm
This trend in reduced permeability with smaller nominal maximum size mixes continues with 12.5 and 9.5 mm mixes that are used for thin overlays. Notice how low the permeability is even at relatively high air voids for the 9.5 mm mix.
This is clear example of why small NMAS mixtures are excellent surfacing materials. If the permeability is reduced, then the aging and durability problems resulting from air and water penetrating the mix can be significantly diminished.

## Slide 43: Construction & Quality Control
Construction
  Production
  Paving
Quality Control
Notes: Next, we will discuss the construction and quality control of thin asphalt overlays.

## Slide 44: Construction - Production
RAP – Process for size and consistency
  Max size < NMAS
Storage and Loading
  Follow normal best practices
Warm Mix
  Increase haul distance
  Pave at cooler temperatures
  Achieve density at lower temperatures
  Extend paving season
  Pave over crack sealer
Notes: RAP should be processed for size and consistency, making sure that the maximum RAP size does not exceed the NMAS of the mix.
Storage of the mix and loader operations should both follow best practices. Like the fine aggregates paving and sloping under the stockpile and covering stockpiles can be very effective in reducing fuel use and increasing productivity.
Warm mix technology can help in the construction of thin overlays by:
increasing the allowable haul distance,
allowing paving and compacting to occur at cooler temperatures, extending the paving season to allow placement of surface mixtures in cooler weather. Paving at cool temperatures is a challenge with thin overlays since the thinner the overlay, the faster the mix will cool. The ability to achieve compaction at cooler temperatures using warm mix is one feature of we need to take advantage of.
Warm mix can also allow paving operations to proceed over crack-sealed pavements without bumps forming.

## Slide 45: Construction – Paving Surface Preparation
Milling
  Remove defects
  Roughen surface
  Improve smoothness
  Provide RAP
  May eliminate need for tack
  Size machinery properly
Tack
  Emulsion or hot asphalt
  Polymer emulsion or unmodified
  Rate: 0.10 to 0.15 gal/sy (undiluted emulsion)
Notes: Milling of the existing pavement is encouraged for a number of reasons. It removes defects that may otherwise reflect through the new overlay and provides an opportunity to improve the smoothness of the final pavement. It roughens the surface which improves the bond between the overlay and the old pavement, and some research has shown it may eliminate the need for a tack coat. It also provides RAP which can be used in future projects. However, it is important to properly size the milling equipment for the pavement structure. A milling machine which is too heavy may structurally damage the pavement.
Tack coats are needed to bond the overlay to the existing pavement which is important to long term performance. Tack coats may be either asphalt emulsions or hot applied tack. The advantage of an emulsion is that it may be applied at ambient or slightly elevated temperatures, where a hot asphalt tack must be applied at elevated temperatures. On the other hand, some practitioners feel that better bonding occurs with the hot applied tack. Some agencies specify the use of a polymer modified tack coat while others are satisfied with the performance of unmodified tack coats. Most specifications require an application rate of between 0.1 and 0.15 gal/sy for undiluted emulsion.

## Slide 46: Construction – Paving Placement and Compaction
Paving
  Best to move continuously
  MTV or windrow can help
  Cooling can be an issue
    1” cools 2X faster than 1.5”
  Warm mix
Compaction
  Seal voids & increase stability
  Low permeability
  No vibratory on < 1”
Notes: In paving, the best strategy to obtain a smooth mat is to move the paver slow but continuously. Develop a plan to balance production, trucking, paving and compaction to keep equipment moving smoothly. If starting and stopping is necessary to deal with interrupted material flow, then it is best to start and stop the paver quickly rather than gradually to maintain a constant mat thickness.
A material transfer vehicle or windrow pickup device can be of help for the delivery and feeding of the asphalt mixture. However, an MTV is not necessary to prevent segregation since the mix is comprised mostly of fine aggregate. When dealing with polymer modified binders, it is also important to minimize the amount of handwork as the material may be very sticky and difficult to rake.
Cooling of the mixture can be an issue for a thin overlay. Keep in mind that a 1 inch mat will cool twice as quickly as a 1.5 inch mat. Again, warm mix technology can help extend the time for compaction of the mix.
Compaction of the mat should be done with the idea of sealing the surface to the penetration of water and air and maximizing the stability of the mix. As discussed earlier, permeability will be decreased with smaller NMAS mixtures even for higher air voids. This will improve the performance of the overlay by reducing the amount of access that air and water have to the mixture. Vibratory compaction should not be used on mats of less than one inch in thickness as this may damage the mat.
As with any pavement construction, uniformity in all aspects of production, transportation, placement, and compaction is key to the success of the pavement.

## Slide 47
Notes: Trackless Tack – breaks in < 10 mins and will not track on trucks ect

## Slide 48
Notes: No butt mill – taper. ¾” loose mat

## Slide 49
Notes: See mat pull at top – caused at start of pull -

## Slide 50
Notes: Irregular mat at the beginning of pull

## Slide 51
Notes: Object in mat – can be caused from truck or hopper or plant chuncks

## Slide 52
Notes: After screed starts floating – don’t stop -

## Slide 53
Notes: Notice no roll push

## Slide 54
Notes: Very little push in front of roller

## Slide 55
Notes: Conventional dumping into paver – or use shuttle buggy with pan -

## Slide 56
Notes: Stay in close with roller due to heat

## Slide 57
Notes: No joint issues

## Slide 59: Quality Control - Plant
Aggregate
  Gradation
  Moisture Content
Mix Volumetrics
  Air Voids
  VMA
  Asphalt Content
  Gradation
Notes: Quality control at the plant should follow normal procedures by checking gradation and moisture content on the incoming aggregate, and normal mix volumetrics on the plant output including air voids, VMA, asphalt content, and gradation.

## Slide 60: Quality Control - Field
Field Density
  Thin-lift NDT gauges OK for > 1” mat
  Cores may not be representative
  Permeability not as big an issue
Ride Quality
  Depends on
    Condition of existing pavement
    Surface preparation
    Overlay thickness
  Specification should be based on existing condition
Notes: Field quality control should also follow normal procedures except that density measurements can be problematic. Thin lift gauges for measuring density should not be used on overlays of less than one inch thick.
Using cores from thin overlays to determine density can also be difficult as the ability to trim the cores for measurement can leave minimal material that may not be representative of the overlay. Coring also blemishes the pavement surface. It may be best to establish a rolling pattern at the beginning of the project and make sure it is followed.
One way to assure you are achieving adequate density is to establish a roller pattern at the beginning of the project. This may be done with thin lift gauges since you are not looking for an absolute density, but whether or not additional passes improve density.
Again, permeability, even for relatively high air voids will be low for small NMAS.
The resulting ride quality on a thin overlay will be dependent upon the condition of the existing pavement, the type of surface preparation allowed, and the overlay thickness. Specifications should focus on a percent improvement in ride quality rather than an absolute number. This will ensure that all that can be done to improve the ride quality will be done.

## Slide 61: Performance
Immediate Benefits
Pavement Life
Economics
Notes: The performance of thin overlays will be discussed in terms of the expected immediate benefits of a thin overlay, the pavement life, and the economics.

## Slide 62: Immediate Benefits
Pavement Condition (Labi et al. (2005))
  18 to 36% decrease in roughness
  5 to 55% decrease in rut depth
  1 to 10% improvement in condition rating
Noise
  Corley-Lay and Mastin (2007): 6.7 dB reduction on overlaid PCC
  FHWA (2005): 5 dB reduction on overlaid PCC in Phoenix
3dB reduction = ½ traffic volume
Notes: Here are some research projects that looked at immediate benefits when using thin overlays.
Labi and his co-workers at Purdue documented an 18 to 36 percent improvement in ride quality after the application of a thin overlay. They also found that rutting was decreased between 5 to 55%, and that there was a 1 to 10 percent improvement in the condition rating of the road.
Noise improvements are noticed immediately on thin overlays. Corley-Lay showed that thin overlays reduced noise levels by 6.7 dB on overlaid concrete pavement in North Carolina, and the FHWA documented a 5 dB reduction on concrete pavements in the Phoenix area that had been overlaid with an asphalt-rubber overlay.
It should be kept in mind that as little as a 3dB reduction in noise is the same as reducing the traffic by half.

## Slide 63: Pavement Life
Location | Traffic | Underlying Pavement | Performance, yrs.
Ohio | High/Low | Asphalt | 16
 | Low | Composite | 11
 | High | Composite | 7
North Carolina | ---- | Concrete | 6 – 10
Ontario | High | Asphalt | 8
Illinois | Low | Asphalt | 7 – 10
New York | ---- | Asphalt | 5 – 8
Indiana | Low | Asphalt | 9 – 11
Austria | High/Low | Asphalt | >10
 | High | Concrete | >8
Georgia | Low | Asphalt | 10
Notes: The expected pavement life of a thin overlay will be determined by traffic loads, the type of underlying pavement and climate among other factors. These studies have documented thin overlay performance in a variety of locations.

## Slide 64: Economics of Preventive Maintenance Treatments

## Slide 65: Thinlay Experience in Oregon
Washington County Case Study

## Slide 66: Murray Blvd.
ADT = 30,000 vehicles per day

## Slide 67: Why Thinlay Overlays? (1” fine graded mix)
Minimize Lane Closures
Appearance and Ride Quality
Added Structural Life
Limited Contractor Availability for Slurry Seals/Micro-Seals
Reduced Risk
Lower Life-Cycle Cost???

## Slide 68: Cost
Thinlay Treatment = $2.53 per square yard
Micro-Surfacing = $1.92 per square yard
32% cost increase

## Slide 69: Life Cycle Costs Estimated in 2001
20 Years, I=4%
Thinlay = $4.24 (based on estimated 10 year life)
Micro Surface = $6.74 (based on experience of 5 year life)
Thinlay Saves $2.50/yd2 in 20 Years and Adds 2” of Structure

## Slide 70: Actual Life Cycle Costs
15 Years, I=4%, Thinlay life = 15 year life
Average micro surfacing life = 5 years
Thinlay = $2.53
Micro Surface = $4.79
Thinlay Saves $2.26/yd2 in 15 Years, adds structure, and provides high serviceability, far less user impact

## Slide 71: Cost Comparison on Murray Blvd. (no discount)
Thin Lift Overlay = $2.53 per square yard
  $0.18 per square yard per year of service
Micro-Surfacing = $1.92 per square yard
  $0.38 per square yard per year of service

## Slide 72: Conclusions - Benefits
Thinlays for Pavement Preservation
  Improve Ride Quality
  Reduce Distresses
  Maintain Road Geometrics
  Reduce Noise
  Low Life Cycle Costs
  Provide Long Lasting Service
  Adds structure
Place before extensive rehab required
Expected performance
  10 years or more on asphalt
  6 to 10 years on PCC
Notes: Thin overlays for pavement preservation are popular due to a number of advantages that have been discussed throughout this presentation. Some of them include better smoothness, reduced surface distress, geometric considerations, noise reduction, lower life cycle cost, and long-lasting performance.
It is best to apply a thin asphalt overlay before extensive rehabilitation is required. This will maximize the performance and minimize the cost.
Thin asphalt overlays can be expected to perform 10 or more years on an existing asphalt pavement and from 6 to 10 years on an existing concrete pavement.