## Slide 1: Lightweight Deflectometer (LWD) Testing for Subgrade Construction Acceptance: INDOT’s Experience
Peter J. Becker, PhD
Indiana Department of Transportation
Division of Research & Development

## Slide 2: Presentation Overview
LWD background
  Performance-based specifications for subgrade construction
  Stiffness-based acceptance testing
  General overview of LWD
  Interpreting LWD test results
LWD use on INDOT contracts
  Initial implementation
  Current specifications
  Future plans

## Slide 3: Lightweight Deflectometer (LWD) Background

## Slide 4: Performance-based Specifications for Subgrade Construction
INDOT has begun implementing performance-based specifications for construction contracts
Performance-based specification definition:
  Quality assurance specification
  Describes desired level of a fundamental engineering property that is a predictor of performance
Resilient modulus (Mr) that describes stiffness is the preferred engineering property for pavement design

## Slide 5: Subgrade Construction Stiffness-based Acceptance Test Methods
Credit: Humboldt Mfg. Co. (https://www.humboldtmfg.com/)
GeoGauge
Credit: Lafayette Instrument Company. (https://lafayetteclegg.com/)
Clegg Hammer
Credit: Zorn Instruments (https://www.zorn-instruments.com/)
Light Weight Deflectometer
Currently used by INDOT for acceptance testing

## Slide 6: LWD Main Components
LWD
0.274 mm
Loading Device
Loading Plate
Data Collector
Drop Weight
Guide Rod
Buffer

## Slide 7: LWD Operation (In General)
LWD
0.274 mm
1. Place loading plate onto ground surface
2. Place loading device onto loading plate
3. Connect data collector to loading plate
4. Lift then release drop weight
  Imparts loading onto loading plate
  Causes loading plate resting on ground surface to deflect vertically
  Amount of deflection depends on stiffness of ground
5. Record measured deflection of loading plate
  Deflection measured using either accelerometer or geophone

## Slide 8: Different LWD manufacturers
Dynatest
Credit: InstroTek (https://www.instrotek.com/)
Credit: Zorn Instruments (https://www.zorn-instruments.com/)
Zorn Instruments
Credit: Olson Instruments (http://www.olsoninstruments.com/)
Olson Instruments
In accordance with ITM 508

## Slide 9: LWD Apparatus in Accordance with ITM 508
≈28-⅜ in. drop height
Loading plate
(11.81 in. diameter)
14.5 psi maximum applied pressure
10 kg drop weight
Accelerometer measuring acceleration with time
Data Collector
Integrates acceleration with respect to time twice to compute deflection
Displays peak deflection in millimeters
Buffer with 354 N/mm spring constant
1,590 lbf peak loading
17 ms pulse duration

## Slide 10: Interpretation of LWD Test Results
Boussinesq’s solution:
x
y
z
x
y
r
z
σz
σθ
σr
τzr
τrz
In Situ Vertical Strain:
ν is Poisson’s ratio
(0.2 to 0.4 typical)
In Situ Stresses:
Vertical Deflection at Surface:
k is applied stress shape factor
E is elastic Modulus
Fo is applied force
ro is loading plate radius
ν is Poisson’s ratio
k is applied stress shape factor
δz is surface deflection
Fo
ro

## Slide 11: Applied Stress Shape Factor (k)
Chart: 
δz
≈0.4δz
Uniform Stress Distribution
Inverse-Parabolic Stress Distribution
Chart: 
 | 34.6712 | 34.6712
Better Assumption

## Slide 12: LWD Elastic Modulus
Chart: Measured Deflection (mm)

## Slide 13: LWD Measurement Influence Depth (MID)
Layered strata
White, D. J., Becker, P., Vennapusa, P. K. R., Dunn, M. J., & White, C. I. (2012). Assessing Soil Stiffness of Stabilized Pavement Foundations. Transportation Research Record, 2335, 99 – 109.
LWD

## Slide 14: Lightweight Deflectometer Implementation on INDOT Contracts

## Slide 15: Initial LWD Implementation
LWD for acceptance testing became standard specification for 2016 contracts
  Intended only for compaction of aggregates (No. 53, No. 73, and Structure Backfill Sizes 1”, 11/2”, and 2”)

## Slide 16: Initial Implementation Required Site Specific Deflection Criteria
Determining Deflection Criteria from Test Pad (ITM 514):
Place aggregate in a 100’ x 20’ area
Compact aggregate with smooth drum vibratory roller (4 passes in vibratory mode, 1 pass in static mode)
Conduct 10 LWD tests across test pad area; determine average deflection
Recompact aggregate with one vibratory roller pass followed by one static roller pass
Conduct 10 LWD tests at same locations as in Step 3; determine average deflection
If there is no change in average deflection, then aggregate is fully compacted; otherwise repeat steps 4 and 5
Maximum deflection for the rest of the contract is the average deflection when the test pad aggregate is fully compacted

## Slide 17: LWD Testing Frequency
One series of LWD tests per 800 tons of aggregate
  LWD test series comprises 3 LWD tests
    2 ft from left edge of construction area
    At middle of construction area
    2 ft from right edge of construction area
One Moisture content test per day
  If deflection is too high and aggregate is wet, wait 24 hours for water to drain

## Slide 18: Current LWD Use at INDOT
With release of the 2018 Standard Specifications, LWD for acceptance testing now applies to subgrade chemical modification in addition to aggregate compaction
14”
4% to 5% Cement or Lime
203.24(b)
Subgrade Treatment Type IB
One LWD test series per 1,400 CY of modified soil

## Slide 19: Why 0.27 mm and 0.30 mm Deflections?
MEPDG Resilient Modulus Inputs
  Cement modified subgrade resilient modulus typically equals 14,500 psi
  Lime modified subgrade resilient modulus typically equals 13,000 psi
Assuming Mr ≈ ELWD
  Cement modified subgrade LWD deflection should equal ≈0.27 mm
  Lime modified subgrade LWD deflection should equal ≈0.30 mm
Fo = 1,589 lbf
ν = 0.30
k = 2
ro = 5.91 in.

## Slide 20: INDOT Intends to Eliminate LWD Test Pads Altogether
SPR-4100
 | Equipment Access Constraints | Target Average LWD Deflection
6 in. No. 53 Aggregate over untreated soil | None | 0.51 mm
 | Rollers prohibited | 0.60 mm
12 in. No. 53 Aggregate over untreated soil | None | 0.34 mm
 | Rollers prohibited | 0.47 mm
Trial LWD Deflection Criteria implemented for contracts during 2019

## Slide 21: Future of Lightweight Deflectometer (LWD) at INDOT

## Slide 22: INDOT Is Improving the LWD Deflection Criteria for Chemically Modified Subgrades (SPR-4230)
Specified chemically modified subgrade resilient modulus used in design
Confirm specified chemically modified subgrade resilient modulus during construction
In situ quality assurance testing
Light weight deflectometer (LWD)
Rapid
Easy to use
Provides stiffness measurement
Goal of SPR-4230:

## Slide 23: Expected outcomes for SPR-4230
Develop empirical model for LWD elastic modulus from applied stress
Predict in situ LWD elastic using empirical model
Chart: Axial Stress, σa (psi)
| 14.417132570871656 | 18.169221247004806 | 21.836686280441867 | 25.6951591052716 | 29.463450460041344
4% PC, OMC, 95% RC | 41021.6501 | 47642.9044 | 56429.795 | 64834.7042 | 66782.6558
4% PC, OMC, 100% RC | 37051.3912 | 41505.8602 | 52110.7926 | 63506.8961
4% PC, 2% wet, 95% RC | 26805.4989 | 32199.9345 | 37206.2764 | 44495.8746 | 52215.8413
4% PC, 2% dry, 95% RC | 14452.1674 | 16625.5413 | 18672.7271 | 20714.6967 | 23227.8589
4% PC, OMC, 90% RC | 13421.5056 | 14845.4307 | 16206.4718 | 15341.3124 | 16695.7584
Chart: σz (psi)
Chart: σr (psi)
Chart: ELWD (psi)
Chart: μεLWD (μin/in)

## Slide 24: Expected outcomes for SPR-4230
Correlate LWD elastic modulus with resilient modulus
Confirm LWD elastic and resilient modulus correlation from FWD testing
Publish findings as Purdue University Joint Transportation Research Program (JTRP) technical report in 2020
Chart: Predicted In Situ LWD Elastic Modulus, *ELWD (psi)
| 16658.357654357729 | 10441.866984792114 | 12142.62152740622 | 24933.989899032054 | 29033.369720984134
 | 13673 | 12608 | 11739 | 15661 | 14607
Chart: LWD Correlated Resilient Modulus, Mr(LWD) psi
| 13371.400105309123 | 14097.463478466861 | 12983.03273546391 | 12127.092124675495 | 14028.473110522144 | 12497.595338350811 | 12571.867488966773 | 12461.330949538282 | 12425.625981462872 | 12190.129416967997 | 11976.827204011739 | 12648.579694081884 | 12035.727820572469 | 10717.205216085868 | 12534.435255409511 | 11603.461131990447 | 12534.435255409511 | 12852.050114427289 | 13319.360539656529 | 12461.330949538282 | 13121.539476372713 | 13649.224028872402 | 13831.858552650685 | 12768.553689939428 | 14168.320806185593 | 13591.148950081928 | 13769.517896532307 | 14908.183849913448 | 13769.517896532307 | 13895.749564194126 | 11438.418966022706 | 12983.03273546391 | 11531.165188189327 | 12534.435255409511 | 13218.458336593927 | 13769.517896532307 | 12609.909546200794 | 12983.03273546391 | 13769.517896532307 | 12355.833069254817
I-65 (Frankfort) | 9389.6246 | 10554.4761 | 8876.6532 | 9181.8554 | 10623.2152 | 11998.8251 | 11792.0341 | 12535.4286 | 11829.6566 | 12092.9863 | 10884.0073 | 10067.3634 | 11728.636 | 10230.4768 | 9011.5657 | 7763.4388 | 7255.3599 | 8540.7583 | 12106.4379 | 9252.0089 | 12159.9403 | 15031.1328 | 15221.3764 | 10662.4785 | 11726.2303 | 10070.447 | 11854.3858 | 10913.0695 | 15081.8566 | 12160.0176 | 9782.8259 | 10944.0296 | 11650.0961 | 8274.3818 | 9229.1182 | 8403.1659 | 9322.762 | 8638.4546 | 11603.8633 | 7174.7962
 | 0 | 30000
I-469 (Fort Wayne) | 11775.0251 | 11621.6329 | 11043.7617 | 11057.2133 | 10385.6843 | 10890.1649 | 11488.0509 | 11436.3177 | 11030.3101 | 11478.0561 | 11969.586 | 22770.3448 | 22825.6798 | 21291.017 | 20191.1198 | 11134.1443 | 9620.7655 | 10136.4651 | 10268.7963 | 10554.8533 | 11316.7765 | 12233.0798 | 12173.6959 | 12959.0956 | 14194.0114 | 13182.8312 | 12666.8076 | 12891.6318 | 14953.6593 | 14824.8563 | 14697.2941 | 14263.082 | 12907.2391 | 12809.5195 | 12728.4466 | 12056.3591 | 15084.3991 | 14643.9787 | 23199.9859
US-6 (Brimfield) | 18891.7725 | 14786.1532 | 12844.8099 | 12434.0139 | 13092.7696 | 14173.6602 | 12829.2026 | 11940.4275 | 11432.0799 | 11940.4275 | 17313.7008 | 17711.1115 | 25658.4052 | 23430.7841 | 18182.3641 | 18083.4719 | 18316.3865 | 16312.7525 | 20456.8292 | 21316.9185
Cleveland Road (South Bend) | 10853.811 | 10699.6916 | 14216.8337 | 13273.2555 | 10366.0865 | 8899.0248 | 11798.0504 | 9669.0599 | 8475.7447 | 11514.5676 | 11124.6859 | 7304.2175 | 8054.8486 | 12303.3565 | 10988.5318 | 9447.2368 | 12216.6619

## Slide 25: Thank you for your attention