## Slide 1: Estimating Camber, Deflection, and Prestress Losses in Precast, Prestressed Bridge Girders, TRC 1606
Ahmed Al-Mohammedi
Micah Hale

## Slide 2: Acknowledgements
Ahmed Al Mohammedi, Graduate Student
Bryan Casillas, Graduate Student
Rick Stanley, ARDOT
Chris McKenney, ARDOT
Patrick Stevens, BGE
Kip Guthrie, BGE
Neil Drews, Coreslab Structures, Tulsa, OK
Pam Gullett, JJ Ferguson Prestress Precast, Greenwood, MS

## Slide 4: Background
The current design methods results in differences between the design and the actual camber.
Excessive camber makes the girder top flanges interfere with the deck thickness and reinforcement, while insufficient camber increases the deck thickness can add extra weight and load on the girders.
These result in :
Cost increase.
Project delay.
Reduce the ride quality of bridges.
Construction problems.

## Slide 5: Background
Why does the design camber not equal the actual camber?
Current Methods for Camber Prediction:
1.80 × initial camber – 1.85 × deflection = camber at erection
2.45 × initial camber – 2.70 × deflection – (others) = final camber
(2) Underestimation of concrete properties.
(3) Inaccurate prediction of strands stress.
The main goal of this project is to improve the accuracy of estimating camber and long-term deflection in precast prestressed concrete girders

## Slide 6: Background
Dead End
Live End
Prestressing Chuck
Cast the concrete
Tension the strand to approximately 0.75fpu
Prestressing Chuck

## Slide 7: Background
Dead End
Live End
Approximately 18 to 24 hours after casting and the concrete has reached sufficient strength, the strands are cut.
The tension force in the strands is now transferred to the concrete. This puts the concrete in compression and the beam shortens.
If the concrete strength is low, then there can be cracking in the end regions, excessive camber, and an increase in prestress losses.

## Slide 8: Background
Dead End
Live End
Camber

## Slide 9: Background
Camber
P
e
What are some factors that effect camber?
Concrete strength/modulus of elasticity. Concrete strength/modulus increases with time. Camber decreases as E increases.
The prestress force. Larger prestress force, more camber. The prestress force decreases over time (prestress losses).
Eccentricity. Larger “e”, larger moment and more camber
Section size (self weight) and section properties (moment of inertia). Larger sections have less camber.
Additional dead load decreases camber.

## Slide 10: Background
All camber/deflection calculations are estimates
  Affected by uncertainties relating to material properties
  Time dependent
  Temperature
  Humidity
  Load application

## Slide 11: Research Plan
Evaluate concrete properties.
Measure strand stress.
Monitor camber in the field.
Evaluate the current design methods.
Several visits were made to two plants which are: (1) Coreslab Structures in Tulsa, OK (2) JJ Ferguson Prestress/Precast in Greenwood, MS.
The objectives from these visits are to:

## Slide 12
Type II
Type III
Coreslab Structures Tulsa, OK
Coreslab Structures Tulsa, OK
Girders are for the job No. CA0901 HWY. 264 – over New Hope Rd. & Blossom Way CR. Benton County, Rogers, AR
Two Type II Girders
  Length = 42ft
  Strands = 10 - 1/2 in. Ø
Two Type III Girders were instrumented.
  Length = 63ft
  Strands = 26 - 1/2 in. Ø
Nine AASHTO girders were instrumented at two precasting plants (Tulsa, OK & Greenwood, MS):

## Slide 13
Type IV
Type VI
Coreslab Structures
Tulsa, OK
J J Ferguson Prestress/Precast Greenwood, MS.
Type VI girders are for job Number CA0907 HWY.112 - I-49 (S), Benton County, Rogers, AR.
Two Type IV Girders
  Length = 91ft
  Strands = 38 - 1/2 in. Ø
Three Type VI Girders
  Length = 109ft
  Strands = 38 - 1/2 in. Ø
Type IV girders are for the Job No. 070282 Hwy 167 in south Arkansas over the Ouachita River, Calion, AR.

## Slide 14: Evaluating Concrete Properties
Concrete was sampled during the casting of each girder. More than 30 cylinders and 6 prisms were cast from each mix. The specimens were brought to the lab the following day and tested for:
1- Compressive strength. 2- Elastic modulus. 3- Unit weight. 4- Creep. 5- Shrinkage.
Coreslab Structure Plant Tulsa, OK
JJ Ferguson Plant Greenwood, MS

## Slide 15: Evaluating Concrete Properties
Shrinkage test
Modulus of Elasticity test
Creep test
Modulus of Elasticity test at JJ Ferguson lab

## Slide 16: Strand Stress
The force in the prestressing strands affect prediction of the camber.
Vibrating Wire Strand Gauges (VWSG) were used to measure the strands stress.
Two gauges were used in each girders. A total of nine girders were instrumented.
VWSG in the top strands.
VWSG locations

## Slide 17
Monitoring camber
The initial camber was measured immediately after release while the girders were still on the prestressing bed and again immediately after moving the girder to storage yard.
Camber was measured multiple times until the girders were shipped to the job site.
Once the girders arrived to the bridge site, camber was measured before and after casting the deck.
Laser level
Humidity and temperature recorder
Laser receiver
Measuring the erection camber using laser level

## Slide 18: Compressive Strength Results
Precasters want the concrete to gain the required release strength in a short period of time in order to cut the strands, move the girder, and start preparing to cast another girder.
The measured compressive strength at release was 27% to as much as 73% higher than the design strength.
Chart: Design versus measured compressive strength at release
| Type II | Type III | Type IV | Type VI
Design Compressive strength at Release | 4500 | 4500 | 5400 | 6000
Measured Compressive Strength at Release | 8653 | 6636 | 7946 | 7590
Ec = 57,000√f’c
Ec = 57,000√4500 = 3820 ksi
Ec = 57,000√8650 = 5300 ksi
 = Pel2/(8EciI)
L = 42 ft, P = 10(190 ksi)(0.153 in2) = 290.7 k
I = 50,980 in4, e = 13.33 in.
 = 0.63 in.
 = 0.45 in.
 = Pel2/(8EciI)
L = 109 ft, P = 38(190 ksi)(0.153 in2) = 1105 k
I = 733,320 in4, e = 33 in.
 = 2.41 in.
 = 2.14 in.
Current Methods for Camber Prediction:
1.80 × initial camber – 1.85 × deflection = camber at erection
2.45 × initial camber – 2.70 × deflection – (others) = final camber

## Slide 19
The ACI 363 equation and the AASHTO LRFD equation underestimated the modulus of elasticity of concrete by 15% to 20%.
Modification factors are proposed in the final report to overcome the underestimation.
Predicted versus measured E at release
Modulus of Elasticity
ACI 363-14
2014 AASHTO LRFD
Chart: AASHTO Type Girders
| Type II | Type III | Type IV | Type VI
Measured MOE at Release | 5720.5 | 5293 | 6173.3333 | 5402.75
Predicted MOE by AASHTO LRFD | 4066.84 | 4066.84 | 4286.8257 | 4695.9823
Predicted MOE by ACI 363 | 3875.6277 | 3875.6277 | 4028.3559 | 4312.4185

## Slide 20: Measured vs Designed Camber:
Chart: Design vs. Measured Camber for Type VI Girders
Measured Camber | 2.1438 | 2.2062 | 3.2188 | 2.2688 | 2.2312 | 2.5125 | 2.5188 | 2.625 | 2.3438 | 2.2812 | 2.3125 | 2.3 | 2.2937 | 2.4625 | 2.375 | 2.5187 | 2.7812 | 2.6188 | 3.0062 | 2.6375 | 2.8563 | 2.7375 | 3.0438 | 2.9937 | 2.7559 | 2.5197 | 2.2047 | 2.6969 | 2.7953 | 2.2638 | 3.0118 | 2.7362 | 2.8346 | 2.9921 | 3.4646 | 3.5433 | 2.9331 | 2.6969 | 2.3819 | 2.6772
Design Erection Camber | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255 | 3.5255
Chart: Design vs. Measured Erection Camber for Type II Girder
Measured Erection Camber | 0.5 | 0.56249 | 0.3125 | 0.4375 | 0.455 | 0.4375 | 0.4375 | 0.5
Design Erection Camber | 0.658 | 0.658 | 0.658 | 0.658 | 0.658 | 0.658 | 0.658 | 0.658
Chart: Design vs. Measured Erection Camber for Type III Girders
Measured Camber on the bridg site | 0.55118 | 0.51181 | 0.80709 | 0.74803 | 0.55118 | 0.66929 | 0.51181 | 0.76772 | 0.74803 | 0.66929 | 0.68898 | 0.51181
Design Camber | 1.524 | 1.524 | 1.524 | 1.524 | 1.524 | 1.524 | 1.524 | 1.524 | 1.524 | 1.524 | 1.524 | 1.524

## Slide 21: Camber at Erection - Summary

## Slide 22: Recommended Changes to Camber Equations
Chart: Number of Type II Girder measured
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
Measured cambers at erection | 0.5 | 0.56249 | 0.3125 | 0.4375 | 0.455 | 0.4375 | 0.4375 | 0.5
ARDOT Prediction | 0.88 | 0.88 | 0.88 | 0.88 | 0.88 | 0.88 | 0.88 | 0.88
Recommended Prediction method | 0.52 | 0.52 | 0.52 | 0.52 | 0.52 | 0.52 | 0.52 | 0.52
Chart: Number of Type III Girder measured
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16
Measured camber at erection | 1.2598 | 0.88583 | 0.90551 | 0.66929 | 0.72835 | 0.96457 | 0.86614 | 0.84646 | 1.1024 | 1.0827 | 1.122 | 1.1024 | 1.063 | 1.4173 | 0.7874 | 0.98688
ARDOT Design Camber | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25 | 2.25
Recommended Prediction method | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2 | 1.2
The recommended method utilizes a single multiplier of 1.4 times the elastic camber (initial camber at release) calculated using gross section properties as shown in the equation below. This multiplier was validated using the camber measurements conducted at girders erection.
Current Methods for Camber Prediction:
1.80 × initial camber – 1.85 × deflection = camber at erection
2.45 × initial camber – 2.70 × deflection – (others) = final camber
1.4

## Slide 23: Recommended Changes to Camber Equations
Chart: Number of Type IV Girder measured
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24
Measured camber at erection | 2.0472 | 0.98425 | 1.1417 | 1.0433 | 1.1417 | 1.2992 | 1.4567 | 1.6732 | 1.1024 | 1.0827 | 1.4961 | 1.7323 | 1.2205 | 1.2 | 1.4173 | 1.8504 | 1.5551 | 1.5157 | 1.3583 | 1.3189 | 1.5157 | 1.5945 | 1.5945 | 1.4173
ARDOT Prediction | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27 | 2.27
Recommended Prediction method | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3 | 1.3
Chart: Number of Type VI Girder
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50 | 51 | 52 | 53 | 54 | 55 | 56 | 57 | 58 | 59 | 60 | 61
Measured cambers at erection | 2.25 | 2.25 | 2.5 | 2.375 | 1.9375 | 2.6875 | 2.4 | 2.4375 | 1.6875 | 2.8346 | 2.5394 | 2.7756 | 1.8898 | 2.2638 | 2.1654 | 2.4606 | 1.1811 | 2.126 | 2.185 | 2.5394 | 1.9291 | 1.9685 | 2.0276 | 2.3031 | 2.2244 | 2.2244 | 2.8346 | 2.5394 | 2.7756 | 1.8898 | 2.2638 | 2.1654 | 2.4606 | 1.9 | 2.126 | 2.185 | 2.5394 | 1.9291 | 1.9824
ARDOT Prediction | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75 | 2.75
Recommended Prediction method | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52 | 2.52

## Slide 24: Prestress Losses
For Type VI girders, the measured prestress losses before deck placement was 34% less than the expected.
  The high compressive strength at release also affects modulus of elasticity.
  The measured elastic shortening losses was very close to the predicted when using transformed section properties.
Chart: Predicted versus Measured Prestress Losses in Type VI Girder
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160
Design losses by 2014 AASHTO refine method | 18.3327 | 24.989 | 29.3309 | 32.3768 | 34.6315 | 36.3679 | 37.7463 | 38.867 | 39.7962 | 40.579 | 41.2476 | 41.8252 | 42.3292 | 42.7729 | 43.1664 | 43.5178 | 43.8336
Measured prestress losses | 29.8635 | 30.4891 | 30.2981 | 29.9945 | 30.1365 | 29.7244 | 28.9188 | 27.9817 | 28.0393 | 25.651 | 21.015 | 20.5043 | 18.5414

## Slide 25: Results
The measured total prestress losses were 146% and 86% less than the design losses calculated by the 2014 AASHTO refined method
The high compressive strength at release decreased the prestress losses.
Elastic shortening losses can be accurately estimated by applying the prestressing force directly to the transformed section properties.
Chart: Predicted versus Measured Prestress Losses in Type II Girder
| 130 | 122 | 109 | 102 | 97 | 90 | 18 | 11 | 1 | 0
Losses in the bottom strands | 11.5653 | 11.8167 | 11.3798 | 10.6959 | 12.411 | 12.8288 | 10.6685 | 9.8415 | 9.3674 | 8.5347
Predicted Using AASHTO 2014 Specifications | 11.6396 | 17.3385 | 21.2553 | 24.099 | 26.2575 | 27.9518 | 29.3171 | 30.4407 | 31.3816 | 32.4975 | 32.8687 | 28.9665 | 29.8074 | 29.9547 | 30.3677 | 30.738 | 31.0718 | 31.3743 | 31.6496 | 31.9013 | 32.1323 | 32.345 | 32.5416 | 32.7237 | 32.893 | 33.0507
Chart: Predicted versus Measured Prestress Losses in Type III Girder
| 110 | 102 | 89 | 82 | 8 | 0.75 | 0.5 | 0.25 | 0
Losses in the bottom strands | 15.1899 | 14.9869 | 16.6146 | 16.6555 | 12.318 | 11.3372 | 11.6783 | 11.9914 | 11.2066
Predicted Using AASHTO 2014 Specifications | 13.6255 | 20.0915 | 24.5223 | 27.7391 | 30.1808 | 32.0974 | 33.6418 | 34.9129 | 35.9773 | 36.7974 | 33.9595 | 34.6357

## Slide 26: Predicted vs Measured Total Prestress Losses
As shown in the percent differences between the measured and predicted prestress losses at the time of deck placement is 146%, 86%, 71%, and 14% for AASHTO Type II, III, IV, and VI girders, respectively.

## Slide 27: Recommended Changes to Modulus of Elasticity Equations
The MOE of concrete is a significant parameter in determining the initial camber and deflection of prestressed concrete girders.
MOE of concrete at release is necessary for estimating both downward and upward defection components of initial camber.
MOE at service is more important for quantifying the downward component which directly affects the long-term deflection.
∆=
∆=
Deflection due to girder self weight
Camber due to prestressing force

## Slide 28
Coarse Aggregate Stiffness Coefficient (K1)
The type and the stiffness of the coarse aggregate affect the modulus of elasticity of concrete. This effect is accounted for by the K1 Coefficient as shown in the equation below:
E = 33 .………………………………....AASHTO LRFD (2012)
ERC Lab
Tulsa, OK
Greenwood, MS

## Slide 29: Coarse Aggregate Stiffness Coefficient (K1)

## Slide 30: Coarse Aggregate Stiffness Coefficient (K1)

## Slide 31: Coarse Aggregate Stiffness Coefficient (K1)
Chart: Concrete mixtures using river gravel (Greenwood, MS)
Measured MOE (ksi) | 5568 | 5367 | 5447 | 7005 | 6021 | 6259 | 6532 | 6427 | 6256 | 6145 | 6430 | 5576 | 6542 | 6140 | 6821 | 6592 | 6311 | 6426 | 5588 | 4286 | 6247 | 6385 | 6154 | 6376 | 7244 | 6775 | 6690 | 5752 | 5700 | 6314 | 6165 | 6237 | 6315 | 6213 | 5655 | 5465 | 6154 | 6073 | 6807 | 6654 | 6967 | 6858 | 4449 | 4191 | 4817 | 4931 | 5787 | 5752 | 5781 | 5472
AASHTO Eq. with K=1.20 (f'c < 6500 psi) | 0 | 1022.645 | 1449.3342 | 1778.8588 | 2058.4335 | 2306.3039 | 2531.8067 | 2740.476 | 2935.91 | 3120.6026 | 3296.3657 | 3464.5641 | 3626.2561 | 3782.2814 | 3933.3193 | 4079.9285 | 4222.5751 | 4361.6524 | 4497.496 | 4630.3946 | 4760.599 | 4888.3288 | 5013.7768 | 5137.1143 | 5258.4934 | 5378.0505 | 5495.9082 | 5612.177 | 5726.9573 | 5840.3403 | 5952.4092 | 6063.2402 | 6172.9033 | 6281.4628 | 6388.9783 | 6495.5046

## Slide 32: Coarse Aggregate Stiffness Coefficient (K1)
The AASHTO LRFD (2014) gives a better estimate for the modulus of elasticity when the concrete compressive strength is higher than 6500 psi. Therefore, it was more realistic to derive two K1 coefficients with a range of applicability below and above 6500 psi. K1 coefficients are summarized in the table below.
Range of Applicability | Crushed limestone (Sulphur Springs, AR ) | River Gravel (Greenwood, MS) | Crushed limestone (Springdale, AR)
f'c < 6.5 ksi | 1.15 | 1.20 | 1.10
f'c > 6.5 ksi | 1.05 | 1.10 | 1.00

## Slide 33: Conclusions
Use measured compressive strengths
  Instead of specified
  Measured release strength were 26 to 80% higher than design strength
Use a multiplier of 1.4 vs 2.45 for final camber
Measure Modulus of Elasticity
  Use recommended K1 values
  Measured E’s at release were 20% to 50% greater than design

## Slide 34: Recommendations
Concrete compressive strength should be taken as:
  7.2 ksi. at release when the specified compressive strength at release is less than 7.0 ksi.
  10% higher than the specified compressive strength at release when the specified compressive strength at release is equal or greater than 7.0 ksi.
The current ARDOT bridge design specification should be adjusted to specify the 28th day concrete compressive strength 50% higher than the design compressive strength at release.
When estimating the initial camber at release camber, use the transformed section properties.

## Slide 35: Questions?
micah@uark.edu