Section 720 of the Standard Specifications for Highway Construction, Edition of 2003, is hereby amended as follows:

The paragraphs in Subsection 720.02(c), Reflectance, are hereby deleted and the following substituted therefore:

The white and yellow films shall comply with ASTM D 4505 reflectivity with Type 1 meeting Reflectivity Level II, and Type 2, 3, and 5 complying with Reflectivity Level I.  Type 3 tapes shall exhibit a minimum retained reflectance value at 1.05° observation and 88.76° entrance angle of 100 mcd/ft2/fc (mcd/m2/lux) for a period of 36 months from the date of installation regardless of daily traffic volumes, when used in longitudinal lines.  Type 4 tape shall comply with the requirements of ASTM D 4592.

Subsection 720.02(d), Acid Resistance is hereby deleted.